認識合金鋼&特殊合金鋼

在碳鋼中加入一種或以上的金屬或非金屬元素，藉以改變碳鋼的機械性質與物理性質，使鋼材獲得不一樣的特性，靈活運用於各種使用需求。

鎳合金鋼

構造用鎳鋼的韌性、耐磨耗及耐蝕性較強，主要是因為鎳元素不與鐵生成碳化物，而是完全固溶於肥粒鐵內。利用這合金元素滲入鋼中，使肥粒鐵強化並進而改變其機械性質的鋼稱為高強度低合金鋼。構造用合金鋼的主要優點為容易淬火，並能改良回火後的機械性質。

鉻鉬合金鋼

鉻鉬鋼是鉻鋼中添加少量的鉬元素所成的合金鋼，其機械性質大致與鎳鉻鋼相近，不會發生硬化脆性，熔接處的晶粒較鎳鉻鋼為細，故熔接性較佳，亦不必經過熱處理。唯此種鋼材當溫度升至400~500 ℃附近時，潛變強度很大，故較適合高溫高壓的機械零件。

鎳鉻鉬合金鋼

鎳鉻鉬鋼是在鎳鉻鋼中加入1.0%以下的鉬元素，可得到強韌的鋼材，是構造用鋼材中最優良的鋼種。因鉬元素的淬火硬化能力大，能回火至相當高的溫度且得到極高的強韌性，改善鎳鉻鋼回火脆性的缺點。主要用於汽車的曲柄軸、連桿、大型軸與齒輪、高強度螺栓及螺帽等。

鎳鉻係不鏽鋼

在鉻系不鏽鋼中提高含鉻量，改善了對硫酸與鹽酸等非氧化性酸類的耐蝕性，此種不鏽鋼稱為鎳鉻系不鏽鋼。其組織在常溫時為沃斯田鐵，質軟韌性好，容易加工且不具磁性。此種不鏽鋼雖無法藉由熱處理來增加其硬度與強度，但在常溫加工中，藉加工硬化效果可直接提高其硬度與強度。

析出硬化型不鏽鋼

是在鐵鉻鎳系合金鋼中再添加其他合金元素，經由沃斯田鐵固溶處理後，再低溫熱處理後，使其析出分散且不損耐蝕性的金屬間化合物，以提高強度與硬度。17-4PH鋼經固溶化處理後急冷等製程，可易於銲接且附有磁性。如再經析出硬化，則可析出微細的銅金屬間化合物，抗拉強度可達1400N/mm2。

高速鋼

常用來製造切削的刀具與工具，硬度相當高，因為適合高速切削而得名。

在加工的過程中，由於高速運轉摩擦產生的高熱並不會影響其切削能力，且其切削能力及硬度反而提高，此種性質稱為高速鋼的紅熱硬度或稱為二次硬化。若從約1200℃冷卻，可得到HRC64~65之硬度，如果再經回火硬度會增加至HRC66~67。

其他材質

我們還能夠生產多種的低&中合金鋼材質，甚至鎢碳鋼、白銅、鈦合金材質等等。詳細的材料特性及介紹，歡迎您聯絡我們，進一步了解與共同研討最適合您產品的材質。

Understanding Alloy Steel & Special Alloy Steel

By adding one or more metals or non-metal elements to carbon steel, we can change the mechanical and physical properties of carbon steel, giving the steel different characteristics for a variety of usage requirements.

Nickel Alloy Steel

Structural nickel steel has stronger toughness, wear resistance, and corrosion resistance, mainly because nickel does not form carbides with iron but is completely dissolved in ferrite. This alloy element is infiltrated into the steel, strengthening the ferrite and thereby changing its mechanical properties. This steel is called high-strength low-alloy steel. The main advantage of structural alloy steel is that it is easy to quench and can improve the mechanical properties after tempering.

Chromium-Molybdenum Alloy Steel

Chromium-molybdenum steel is an alloy steel formed by adding a small amount of molybdenum element to chromium steel. Its mechanical properties are roughly similar to those of nickel-chromium steel. It does not exhibit hardened brittleness, and the grains at the weld are finer than those of nickel-chromium steel, hence it has better weldability and does not require heat treatment. However, when the temperature of this steel rises to around 400~500℃, the creep strength is very high, making it more suitable for high-temperature, high-pressure mechanical parts.

Nickel-Chromium-Molybdenum Alloy Steel

Nickel-chromium-molybdenum steel is made by adding less than 1.0% of molybdenum element to nickel-chromium steel. It results in a strong and tough steel, the best steel type for structural use. Due to the high hardening ability of molybdenum, it can be tempered to quite high temperatures to get extremely high toughness, overcoming the temper brittleness drawback of nickel-chromium steel. It is mainly used for automobile crankshafts, connecting rods, large shafts and gears, high-strength bolts, and nuts, etc.

Nickel-Chromium Stainless Steel

By increasing the chromium content in chromium stainless steel, the corrosion resistance to non-oxidizing acids such as sulfuric acid and hydrochloric acid is improved. This type of stainless steel is called nickel-chromium stainless steel. Its structure at room temperature is austenite, which is soft and tough, easy to process, and non-magnetic. Although this stainless steel cannot increase its hardness and strength through heat treatment, its hardness and strength can be directly improved through work hardening during room temperature processing.

Precipitation Hardening Stainless Steel

This is a type of stainless steel where other alloy elements are added to the iron-chromium-nickel alloy steel. After austenite solution treatment and then low-temperature heat treatment, it precipitates dispersed intermetallic compounds that do not damage corrosion resistance, thereby improving strength and hardness. 17-4PH steel, after solution treatment and rapid cooling processes, is easy to weld and has magnetism. If it goes through precipitation hardening, it can precipitate fine copper intermetallic compounds, and the tensile strength can reach 1400N/mm2.

High-Speed Steel

This type of steel is often used in the manufacturing of cutting tools due to its high hardness, hence its name "high-speed steel" for its suitability in high-speed cutting applications. During the machining process, the high heat produced by rapid rotational friction does not affect its cutting ability. On the contrary, both its cutting ability and hardness are enhanced, a characteristic known as the red hardness or secondary hardening of high-speed steel. If cooled from around 1200℃, it can achieve a hardness of HRC64 to 65. After tempering, the hardness can further increase to HRC66 to 67.

Other Materials

We can also produce a variety of low & medium alloy steel materials, and even tungsten carbide steel, white copper, titanium alloy materials, and more. For detailed material characteristics and introductions, please feel free to contact us. We are happy to further discuss and find the most suitable material for your product.